3.1 Exterior Schedule (Premium Plus)

A. Concrete, Plaster and Masonry – 100% Acrylic Flat

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	2000 Duratone 100% Acrylic Flat Finish

Third Coat:	2000 Duratone 100% Acrylic Flat Finish

B. Concrete Masonry Unit (CMU) – 100% Acrylic Flat

First Coat:	018 100% Acrylic Block Filler

Second Coat:	2000 Duratone 100% Acrylic Flat Finish

Third Coat:	2000 Duratone 100% Acrylic Flat Finish

C. Cement Plaster (Stucco) – 100% Acrylic Flat

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	2000 Duratone 100% Acrylic Flat Finish

Third Coat:	2000 Duratone 100% Acrylic Flat Finish

D. Wood – 100% Acrylic Solid Body Stain

Two Coats:	3000 Acribond 100% Acrylic Solid Body Stain

E. Wood – 100% Acrylic Enamel - Eggshell Finish

First Coat:	4200 Terminator II Acrylic Epoxy Primer / Stain Blocker

Second Coat:	8300 Carefree Eggshell 100% Acrylic Enamel

Third Coat:	8300 Carefree Eggshell 100% Acrylic Enamel

3.1 Exterior (Premium Plus) (Continued)

F. Wood – 100% Acrylic Enamel – Semi-Gloss Finish

First Coat:	4200 Terminator II Acrylic Epoxy Primer / Stain Blocker

Second Coat:	8400 Carefree Semi-Gloss 100% Acrylic Enamel

Third Coat:	8400 Carefree Semi-Gloss 100% Acrylic Enamel

G. Wood – 100% Acrylic Enamel – Gloss Finish

First Coat:	4200 Terminator II Acrylic Epoxy Primer / Stain Blocker

Second Coat:	8500 Carefree Gloss 100% Acrylic Enamel

Third Coat:	8500 Carefree Gloss 100% Acrylic Enamel

H. Metal: Ferrous – Satin Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

I. Metal Ferrous – Semi-Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9700 Protec Alkyd Emulsion Semi-Gloss Enamel

J. Metal: Ferrous – Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9700 Protec Alkyd Emulsion Semi-Gloss Enamel

3.1 Exterior (Premium Plus) (Continued)

K. Metal: Non-Ferrous (Galvanized) Satin Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

L. Metal: Non-Ferrous (Galvanized) Semi-Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

M. Metal: Non-Ferrous (Galvanized) Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

Third Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

N. Stucco, Concrete, Plaster – 100% Acrylic Hi-Build Elastomeric

First Coat:	4600 Uniprime II Acrylic Epoxy Masonry Primer

Finish Coat(s):	500 Solotex 100% Acrylic Hi-Build Elastomeric

(15-18 Mils DFT)

3.1 Exterior (Premium Plus) (Continued)

O. Concrete Block Masonry (CMU) - 100% Acrylic Hi-Build Elastomeric

First Coat:  018 100% Acrylic Block Filler

Finish Coat(s):	500 Solotex 100% Acrylic Hi-Build Elastomeric

(15-18 Mils DFT)

P. Stucco, Concrete, Plaster – 100% Acrylic Medium-Build Elastomeric

First Coat:  4600 Uniprime II Acrylic Epoxy Masonry Primer

Finish Coat(s): 1900 Weathermaster 100% Acrylic Medium-Build Elastomeric (6-8 Mils DFT)

Q. Concrete Block Masonry (CMU) – 100% Acrylic Medium Build Elastomeric

First Coat:	018 100% Acrylic Block Filler

Finish Coat(s): 1900 Weathermaster 100% Acrylic Medium-Build  Elastomeric (6-8 Mils DFT)

3.2 Interior Schedule (Premium Plus)

A. Gypsum Board Surfaces (Drywall) Acrylic Flat Finish

First Coat:	1100 Hi-Build PVA Sealer

Second Coat:	8100 Carefree Acrylic Flat Finish

Third Coat:	8100 Carefree Acrylic Flat Finish

B. Gypsum Board Surfaces (Drywall) Acrylic Low Sheen Finish

First Coat:	1100 Hi-Build PVA Sealer

Second Coat:	8200 Carefree Velvasheen Acrylic Low Sheen

Third Coat: 	8200 Carefree Velvasheen Acrylic Low Sheen

3.2 Interior Schedule (Premium Plus) (Continued)

C. Gypsum Board Surfaces (Drywall) 100% Acrylic Eggshell Finish

First Coat:	1100 Hi-Build PVA Sealer

Second Coat:	8300 Carefree 100% Acrylic Eggshell Finish

Third Coat:	8300 Carefree 100% Acrylic Eggshell Finish

D. Gypsum Board Surfaces (Drywall) 100% Acrylic Semi-Gloss Finish

First Coat:	1100 Hi-Build PVA Sealer

Second Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

Third Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

E. Concrete, Plaster, Masonry – Acrylic Flat Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	8100 Carefree Acrylic Flat Finish

Third Coat:	8100 Carefree Acrylic Flat Finish

F. Concrete, Plaster, Masonry – Acrylic Low Sheen Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	8200 Carefree Velvasheen Acrylic Low Sheen Finish

Third Coat:	8200 Carefree Velvasheen Acrylic Low Sheen Finish

3.2 Interior Schedule (Premium Plus) (Continued)

G. Concrete, Plaster, Masonry – 100% Acrylic Eggshell Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	8300 Carefree 100%Acrylic Eggshell Finish

Third Coat:	8300 Carefree 100%Acrylic Eggshell Finish

H. Concrete, Plaster, Masonry – 100% Acrylic Eggshell Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	8300 Carefree 100%Acrylic Eggshell Finish

Third Coat:	8300 Carefree 100%Acrylic Eggshell Finish

I. Concrete, Plaster, Masonry – 100% Acrylic Semi-Gloss Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	8300 Carefree 100%Acrylic Semi-Gloss Finish

Third Coat:	8300 Carefree 100%Acrylic Semi-Gloss Finish

J. Concrete Masonry Unit (CMU) Acrylic Flat Finish

First Coat:	018 100% Acrylic Block Filler

Second Coat:	8100 Carefree Acrylic Flat Finish

Third Coat:	8100 Carefree Acrylic Flat Finish

K. Concrete Masonry Unit (CMU) Acrylic Low Sheen Finish

First Coat:	018 100% Acrylic Block Filler

Second Coat:	8200 Carefree Velvasheen Acrylic Low Sheen Finish

Third Coat:	8200 Carefree Velvasheen Acrylic Low Sheen Finish

3.2 Interior Schedule (Premium Plus) (Continued)

L. Concrete Masonry Unit (CMU) 100% Acrylic Eggshell Finish

First Coat:	018 100% Acrylic Block Filler

Second Coat:	8300 Carefree 100% Acrylic Eggshell Finish

Third Coat:	8300 Carefree 100% Acrylic Eggshell Finish

M. Concrete Masonry Unit (CMU) 100% Acrylic Semi-Gloss Finish

First Coat:	018 100% Acrylic Block Filler

Second Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

Third Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

N. Wood – 100% Acrylic Eggshell Finish

First Coat:	8000 Carefree Prime-Zall Universal Primer

Second Coat:	8300 Carefree 100% Acrylic Eggshell Finish

Third Coat:	8300 Carefree 100% Acrylic Eggshell Finish

O. Wood – 100% Acrylic Semi-Gloss Finish

First Coat:	8000 Carefree Prime-Zall Universal Primer

Second Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

Third Coat:	8400 Carefree 100% Acrylic Semi-Gloss Finish

P. Metal: Ferrous – Satin Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

3.2 Interior Schedule (Premium Plus) (Continued)

Q. Metal: Ferrous – Semi-Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

R. Metal: Ferrous – Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

Third Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

S. Metal: Non-Ferrous (Galvanized) Satin Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

T. Metal: Non-Ferrous (Galvanized) Semi-Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

3.2 Interior Schedule (Premium Plus) (Continued)

U. Metal: Non-Ferrous (Galvanized) Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

Third Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

End of Section