3.1 Exterior Schedule (Premium)

A. Concrete, Plaster and Masonry – 100% Acrylic Flat

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	3000 Acribond 100% Acrylic Flat Finish

Third Coat:	3000 Acribond 100% Acrylic Flat Finish

B. Concrete Masonry Unit (CMU) – 100% Acrylic Flat

First Coat:	040 Acrylic Block Filler

Second Coat:	3000 Acribond 100% Acrylic Flat Finish

Third Coat:	3000 Acribond 100% Acrylic Flat Finish

C. Cement Plaster (Stucco) – 100% Acrylic Flat

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	3000 Acribond 100% Acrylic Flat Finish

Third Coat:	3000 Acribond 100% Acrylic Flat Finish

D. Wood – 100% Acrylic Solid Body Stain

Two Coats:	3000 Acribond 100% Acrylic Solid Body Stain

E. Wood – 100% Acrylic Enamel - Eggshell Finish

First Coat:	4200 Terminator II Acrylic Epoxy Primer / Stain Blocker

Second Coat:	7500 Acriglo Eggshell Acrylic Enamel

Third Coat:	7500 Acriglo Eggshell Acrylic Enamel

3.1 Exterior (Premium) (Continued)

F. Wood –100% Acrylic Enamel – Semi-Gloss Finish

First Coat:	4200 Terminator II Acrylic Epoxy Primer / Stain Blocker

Second Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

Third Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

G. Metal: Ferrous – 100% Acrylic Enamel - Eggshell Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	7500 Acriglo Eggshell Acrylic Enamel

Third Coat:	7500 Acriglo Eggshell Acrylic Enamel

H. Metal Ferrous – 100% Acrylic Enamel – Semi-Gloss Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

Third Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

I. Metal: Non-Ferrous (Galvanized) 100% Acrylic Enamel - Eggshell Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	7500 Acriglo Eggshell Acrylic Enamel

Third Coat:	7500 Acriglo Eggshell Acrylic Enamel

3.1 Exterior (Premium) (Continued)

J. Metal: Non-Ferrous (Galvanized) 100% Acrylic Enamel – Semi-Gloss Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

Third Coat:	7000 Acriglo Semi-Gloss Acrylic Enamel

K. Stucco, Concrete, Plaster – 100% Acrylic Medium-Build Elastomeric

First Coat:	4700 Tilt-Up Primer

Finish Coat(s):	1900 Weather Master 100% Acrylic Medium Build

(6-8 Mils DFT)

L. Concrete Block Masonry (CMU) - 100% Acrylic Medium-Build Elastomeric

First Coat:	040 Acrylic Block Filler

Finish Coat(s): 1900 Weather Master 100% Acrylic Medium Build

(6-8 Mils DFT)

M. Stucco, Concrete, Plaster – 100% Acrylic Medium-Build Elastomeric

First Coat:	4700 Tilt-Up Primer

Finish Coat(s):	1900 Weathermaster 100% Acrylic Medium-Build

(6-8 Mils DFT)

N. Concrete Block Masonry (CMU) – 100% Acrylic Medium Build Elastomeric

First Coat:	040 Acrylic Block Filler

Finish Coat(s):	1900 Weathermaster 100% Acrylic Medium Build

(6-8 Mils DFT)

3.2 Interior Schedule (Premium)

A. Gypsum Board Surfaces (Drywall) Acrylic Flat Finish

First Coat:	155 Seal Kote PVA Sealer

Second Coat:	7100 Acriglo Flat Finish

Third Coat:	7100 Acriglo Flat Finish

B. Gypsum Board Surfaces (Drywall) 100% Acrylic Low Sheen Finish

First Coat:	155 Seal Kote PVA Sealer

Second Coat:	1750 Acriglo 100% Acrylic Velvasheen Finish

Third Coat: 	1750 Acriglo 100% Acrylic Velvasheen Finish

C. Gypsum Board Surfaces (Drywall) 100% Acrylic Eggshell Finish

First Coat:	155 Seal Kote PVA Sealer

Second Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

Third Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

D. Gypsum Board Surfaces (Drywall) 100% Acrylic Semi-Gloss Finish

First Coat:	155 Seal Kote PVA Sealer

Second Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

Third Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

E. Concrete, Plaster, Masonry – Acrylic Flat Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	1000 Duraglide Acrylic Flat Finish

Third Coat:	1000 Duraglide Acrylic Flat Finish

3.2 Interior Schedule (Premium) (Continued)

F. Concrete, Plaster, Masonry – 100%Acrylic Low Sheen Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	1750 Acriglo 100% Acrylic Velvasheen Finish

Third Coat:	1750 Acriglo 100% Acrylic Velvasheen Finish

G. Concrete, Plaster, Masonry – 100% Acrylic Eggshell Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	7500 Acriglo 100%Acrylic Eggshell Finish

Third Coat:	7500 Acriglo 100%Acrylic Eggshell Finish

H. Concrete, Plaster, Masonry – 100% Acrylic Semi-Gloss Finish

First Coat:	4600 Uniprime II Acrylic Epoxy Primer

Second Coat:	7000 Acriglo 100%Acrylic Semi-Gloss Finish

Third Coat:	7000 Acriglo 100%Acrylic Semi-Gloss Finish

I. Concrete Masonry Unit (CMU)

First Coat:	040 Block Kote Acrylic Block Filler

Second Coat:	1000 Duraglide Acrylic Flat Finish

Third Coat:	1000 Duraglide Acrylic Flat Finish

J. Concrete Masonry Unit (CMU) Acrylic Low Sheen Finish

First Coat:	040 Block Kote Acrylic Block Filler

Second Coat:	1750 Acriglo 100% Acrylic Velvasheen Finish

Third Coat:	1750 Acriglo 100% Acrylic Velvasheen Finish

3.2 Interior Schedule (Premium) (Continued)

K. Concrete Masonry Unit (CMU) 100% Acrylic Eggshell Finish

First Coat:	040 Block Kote Acrylic Block Filler

Second Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

Third Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

L. Concrete Masonry Unit (CMU) 100% Acrylic Semi-Gloss Finish

First Coat:	040 Block Kote Acrylic Block Filler

Second Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

Third Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

M. Wood – 100% Acrylic Eggshell Finish

First Coat:	4200 Terminator II Primer

Second Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

Third Coat:	7500 Acriglo 100% Acrylic Eggshell Finish

N. Wood – 100% Acrylic Semi-Gloss Finish

First Coat:	4200 Terminator II Primer

Second Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

Third Coat:	7000 Acriglo 100% Acrylic Semi-Gloss Finish

O. Metal: Ferrous – Satin Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

3.2 Interior Schedule (Premium) (Continued)

P. Metal: Ferrous – Semi-Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Q. Metal: Ferrous – Gloss Enamel Finish

First Coat:	9600 Protec Alkyd Emulsion Metal Primer

Second Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

Third Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

R. Metal: Non-Ferrous (Galvanized) Satin Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9700 Protec Alkyd Emulsion Satin Enamel

Third Coat:	9700 Protec Alkyd Emulsion Satin Enamel

S. Metal: Non-Ferrous (Galvanized) Semi-Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

Third Coat:	9800 Protec Alkyd Emulsion Semi-Gloss Enamel

3.2 Interior Schedule (Premium) (Continued)

T. Metal: Non-Ferrous (Galvanized) Gloss Enamel Finish

Pretreatment:	Krud Kutter Metal Clean & Etch

First Coat:	4800 Metal Pro Acrylic Metal Primer

Second Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

Third Coat:	9900 Protec Alkyd Emulsion Gloss Enamel

End of Section